## Slide 1: 3D Printing Microwave Antennas

## Slide 2: Hello!
I am Glenn Robb
KS4VA
Principal Engineer at Antenna Test Lab Co.
Glenn@AntennaTestLab.com

## Slide 3: I test antennas for a living
… and I it !
I’m lucky to own a well equipped commercial laboratory.
Today I’m showing you how to 3D print great microwave antennas.

## Slide 4: Let’s 3D Print Some Antennas
Standard 3D Printers
Inexpensive plastic filament
Smooth the active surfaces
Spray coat
Optional VSWR testing
Why ?
Inexpensive way to learn, create, and modernize
Create, innovate, and iterate
Get working useable parts
Shareable and reproduceable
Quickly go beyond machining and metal folding
Curves and crazy shapes 😁

## Slide 5: What We Won’t Cover
3D Modelling Basics
Software, there is lots of free stuff
I like Sketchup Make 2017
“Slicing software”
Design and simulation
3D Printing
Printer models and machines
Filaments and plastics
Printing techniques

## Slide 6: The Experiment
Duplicate and test known microwave antennas from 2 to 40 GHz

## Slide 7
Straight To It !!!
Made two X-Band 15 dBi standard gain horn antennas. Used two types of spray on conductive coatings. Then in to the chamber

## Slide 8
X-Band
Print

## Slide 9: Initial Results
😭
5.6 dBi

## Slide 10
Measured
Results

## Slide 11: First Horn Antenna Performance
The Bad
We made a 15 dBi standard gain horn that only had 5.6 dBi gain
But Notice
Spherically integrating the 3D pattern shows average gain was -9.2 dBi or 12% radiation efficiency
Red
Therefore directivity is 14.8 dB
Pattern and beam-width look good
So the horn is working but is has a built in 9.2 dB “attenuator” 😁

## Slide 12: So What Went Wrong?
The horn has the correct standard gain directions
The surface coating conductivity is very high
The swept return loss is better than 20 dB
VSWR sweep lower than 1.2:1
?

## Slide 14: It has to be Surface “Roughness”
Smooth It
We figured out a way to smooth the plastic surface (lots more on this later) and re-coated it.
Re-Test It
Eureka! Now we have a 15 dBi standard gain horn with 15 dBi of gain!

## Slide 16: So How Well Does it Work?

## Slide 17: How Do I Smooth My 3D Print?
ANY WAY YOU WANT TO !

## Slide 18: We Tried 4 Ways
Chemicals
Solvents can soften plastic and scrubbing works quickly
Sand It
Sandpaper will do the job just fine
File It
Handheld files do a great job on smaller horns and details
Epoxy Paint
Brush on thick epoxy to cover surface roughness

## Slide 19: Solvent Smoothing
Works the fastest for large surfaces
Acetone for ABS
Dichloromethane (methylene chloride) for PLA

## Slide 20: Stay Safe
Breathe
Work outdoors
Respirator
Hands
Rated chemical rubber gloves
Work-gloves over top
Eyes
You’ll be brushing and splashing !
Regulations
Dichloromethane was the poisonous ingredient in paint stripper
☠☠☠☠☠☠

## Slide 21: Practical Solvent Smoothing
Paint Tray
Work in a metal paint tray outdoors
Scrub
Coarse steel wool or a metal pot scrubber
Paint Brush
Disposable bristle brushes (not plastic) and a bottle brush
Join Parts
When your parts are “tacky” you can solvent weld them

## Slide 22: Sand / File
Works best for small parts and details
Plastic is easy to file
File sets in all shapes and sizes
No chemicals of glue
Best above 26 GHz

## Slide 23: Epoxy Coat
No harsh chemicals,
Not for small details
A thick coating to cover roughness
Use indoors, safer than solvent
Brand XTC-3D from
www.smooth-on.com

## Slide 24: Prime the Epoxy
The metalized paint won’t stick to shiny epoxy
You can sand your cured epoxy
Or prime with a plastic primer
Krylon Fusion worked well
Lowes / Home Depot

## Slide 25: Metalization
We tried these two commonly available “shield paints”
MG Chemicals (even on Amazon)
Nickel “841 Super Shield” was not so good
Silver/copper “843AR Super Shield” was flawless
Use like any other spray paint
Two coats, don’t worry about drips

## Slide 26: Testing
How do I know it works ?
A standard gain horn is a “recipe”
Dimensions are easy
Smooth it / Use the Cu/Ag spray
You “should” be good to go
You don’t need an anechoic chamber

## Slide 27: Short It Out!
How do I know it works ?
Return loss test your horn antenna
An open horn has high return loss
But it could be a good or lossy horn
Short the horn with aluminum foil
Good horn will have low R/L
Lossy horn has losses EXPOSED !

## Slide 28: Baked Potato Method
Similar to the
Wheeler Cap Method

## Slide 29: See For Yourself!

## Slide 30: Let’s See Some Pictures

## Slide 35: Thanks!
Any questions?
You can find me at:
Glenn@AntennaTestLab.com
File downloads at:
www.AntennaTestLab.com/3Dprinting
Thanks to Paul Wade for his help and encouragement