## Slide 1
Wayne Getchell VE3CZO
Soldering
SMT

## Slide 2: SMT Soldering Tool Suite
Basic Tools
  Soldering Stations (s)
    Soldering iron tips
    Stand
    Sponge, tip cleaner
  Water bottle with distilled water
  Isopropanol 99% with drop dispenser bottle
  Cotton swabs –’Q-Tips’
  Liquid no clean flux with flux dispenser bottle
  Solder
    Either tin lead or lead free (higher melting point)
      No clean flux core is ideal
    Small diameter .01 to .020 inches (0.25 to 0.5 mm)

## Slide 3: SMT Soldering Tool Suite
Basic Tools (cont’d)
  Tweezers – length grip to tip – relaxed opening width – tip shape –heft
  Lamp loupe – large glass with three diopter optics or head band magnifying glass (personal preference)
  PCB holder / vice – low profile so hands can rest on bench for support and still reach PCB working area – alternately hand rest area on holder
  Electrostatic Discharge (ESD) protection
    Mat and or wrist strap to ground

## Slide 4: Tool Tips
Soldering Irons – what to look for…
  Controlled tip temperature
  Short tip to grip distance
  Stable fairly heavy stand with tip cleaning sponge
  Replaceable tips
  Short in length Chisel tip
    about 1.2 -1.5mm end
  Bent round tip with point under 1mm.

## Slide 5: Soldering Stations
Soldering Stations I like
  Personal preference – both produce sufficient heat for most applications (tough sledding in large ground planes with lead free solder)
  Cooper tools Weller WD1 with WP80 pencil
    Low cost replaceable tips LTB, LTC, LTHX
  Metcal STS. STSS, or SP200
    Very short tip to grip distance
    Small tip diameter .020 with bent round tip STTC-144
  Both can be found on eBay for typically under $100 or new from about $230. Active Components Ottawa stock.

## Slide 6: Other Tools
Magnifier Lamp
  Craftex B2462 from Busy Bee Machine Tools 3 diopter 7” lens with dust cover. 32W fluorescent tube($60.00)
Tweezers
  TNI-U TU-14B from eBay via BudgetGadgetsSuperStore Hong Kong ($4.00)

## Slide 7: Other Tools
Solder Flux
  No clean similar to Kester 851
  Flux dispenser bottle
  Not always used especially on tinned PCB’s but it’s extremely good at getting solder to wet on harder to solder surfaces
Bench top Smoke Absorber
  I don’t use one but probably should. Like the smell of solder fumes.

## Slide 8: Soldering Process
General Stuff
  Set the soldering iron tip temperature to about 300 C. This is sufficient heat for all tin lead and lead free solders. Too much head can damage the board and parts.
  The soldering iron tip must be well tinned for good heat conduction
Non-tinned boards
  Two and three lead devices
    Wipe area clean with swab and isopropanol
    Apply a drop of flux to one PCB land
    Apply a very small amount of solder to ‘wet’ the land
    Position the part and heat the ‘wetted’ land to tack the part down
    The part should now be in position and affixed to the board

## Slide 9: Soldering Process (cont’d)
Non-Tinned Boards (cont’d)
    Solder the other lead
      Place solder against the part covering half to 2/3 of the part’s end
      Bring the soldering iron to the PCB land and melt the solder to get good reflow
      Avoid hitting the part with your soldering iron tip or you may move it
      Be quick. Long applications of heat will melt solder at both ends of the device and through surface tension you may end up pulling the device off the board especially with smaller 0603 and 0402 parts
    Solder all other leads

## Slide 10: Soldering Process (cont’d)
Non-Tinned Boards
  Multi lead parts
    Tack two diagonally opposite leads first
    Insure all leads align with the PCB pads reposition the part as necessary to get best alignment
    Solder the remaining leads
Tinned Boards
  In most cases there is no need to wet the land with solder flux before tacking the first lead to the PCB

## Slide 11: De-Soldering
Two Leaded Components
  Use two soldering irons one on each end of the part
    Small parts will ‘stick’ to one of the irons so lifts off the board easily
    Larger parts can be lifted off the board by gripping it between the soldering irons
Multi-Leaded Parts
  Heat Gun
    Tends to heat up all surrounding parts so is useful to cut a hole in a piece of aluminium foil and use it as a mask to protect other parts. Cost around $40
  Hot Air Rework Station
    Better solution provides a variety of heat nozzles with different opening diameters to contain and direct heat, temperature and air flow controlled. Cost $100 & up
    I use an Aoyue 852A++ cost $150.
  Technique is the same for both. Apply heat on the solder joints moving the wand around until solder melts at all leads. Pick device from the PCB with a pair of tweezers or vacuum.

## Slide 12: De-Soldering (cont’d)
Cleaning Up
  De-Soldering Braid removes excess solder
    Resin impregnated copper braid with brand names like Soder-Wick, Dri-Wick, Pro-Wick etc.
    Best widths 0.8mm (.030”) for SDM 2mm (.075”) for bigger stuff
    Place the braid over the area with the excess solder then place the soldering iron on the braid. Let the soldering thoroughly heat the braid, don’t rub the area. The excess solder will wick into the braid
  Isopropanol 99% soaked into a cotton swab removes solder flux

## Slide 13: What to avoid
Tools & Supplies
  Soldering Irons with long tip to grip distances
  Rosin based flux – leaves a gooey mess under the part that’s hard to clean
  Trying to apply liquid no-clean flux without a proper dispenser – the stuff has low viscosity, runs all over the place. You’ll waste a lot of material, and it doesn’t smell nice.